## Slide 1
Comparison Between InertSustain C18 and Commercially Available ODS Columns

## Slide 2
Brand Name | Column Size (mm) | Particle Size (μm) | Surface Area (m2/g) | Pore Size (Å) | Pore Volume (mL/g) | Carbon Loading (%)
InertSustain C18 | 2.1×150 | 3 | 350 | 100 | 0.85 | 14
Brand-A CAPCELL PAK C18 MGⅢ, Shiseido | 2.0×150 | 3 | 260 | 100 | 0.91 | 15
Brand-B YMC-Triart C18, YMC | 2.0×150 | 3 | － | 120 | － | Approx. 20
Brand-C L-column2 ODS, CERI | 2.1×150 | 3 | 340 | 120 | 1.10 | 17
Brand-D Cadenza CD-C18, Imtakt | 2.0×150 | 3 | － | 120 | － | －
Brand-E Gemini-NX 3u C18, Phenomenex | 2.0×150 | 3 | 375 | 110 | 1.10 | 14
Brand-F Luna 3u C18(2), Phenomenex | 2.0×150 | 3 | 400 | 100 | － | 17.5
Brand-G X SELECT CSH C18, Waters | 2.1×150 | 3.5 | 390 | 105 | 1.10 | 15
Brand-H XBridge C18, Waters | 2.1×150 | 3.5 | 185 | 135 | 0.74 | 18
Brand-I ZORBAX Eclipse Plus C18, Agilent | 2.1×150 | 3.5 | 160 | 95 | － | 8
Inertsil ODS-3 | 2.1×150 | 3 | 450 | 100 | 1.05 | 15
Inertsil ODS-4 | 2.1×150 | 3 | 450 | 100 | 1.05 | 11
Comparison Table

## Slide 3
Conditions
Eluent :A) CH3CN
B) 25 mM K2HPO4 (pH 7.0, KH2PO4)
A/B = 30/70
Flow Rate : 0.2 mL/min
Col. Temp. : 40 ℃
Detection : UV 230 nm
Sample ： 1:Uracil 2:Pyridine 3:Phenol
4:Berberine hydrochloride 5:Dextromethorphan
Conditions
Eluent :A) CH3CN
B) 25mM K2HPO4 (pH 7.0, KH2PO4)
A/B = 60/40
Flow Rate : 0.3 mL/min
Col. Temp. : 40 ℃
Detection : UV 220 nm
Sample ： 1: Chlorpheniramine 2: Triprolidine
3: Homochlorcyclizine 4: Hydroxyzine
5: Clemastine
The following are antidepressants, which are also strong basic compounds. Poor endcapped columns will show tailing or some even may show different elution pattern. All compounds except for Hydroxyzine tends to elute later.
Conditions
Eluent : CH3OH/H2O = 80/20
Flow Rate : 0.3 mL/min
Col. Temp. : 40 ℃
Detection : UV 254 nm
Sample ： 1: Uracil 2: Toluene 3: Ethylbenzene
4: Propylbenzene 5: n-Butylbenzene
6: n-Amylbenzene
Alkyl benzene is introduced to measure the retentivity of each column.
Dextromethorphan is a strong basic compound.
Severe tailing can be confirmed when the packing material contains residual silanol groups.
R： 2. Toluene
3. Ethylbenzene
4. Propylbenzene
5. Butylbenzene
6. Amylbenzene
4. Berberine hydrochloride
5. Dextromethorphan
1. Chlorpheniramine
2. Triprolidine
3. Homochlorcyclizine
4. Hydroxyzine
5. Clemastine
Basic Compound Test (1)
Hydrophobicity Test
Basic Compound Test (2)
Explanation of Analytical Tests and Conditions
Notes: 3

## Slide 4
Conditions
Eluent :A) CH3CN
B) 0.1%H3PO4
A/B = 40/60
Flow rate : 0.2 mL/min
Col. Temp. : 40 ℃
Detection : UV 254 nm
Inject Vol. ： 1 μL, 10 ppm
Sample ： 1: β-Thujaplicin (Hinokitiol)
Sharp peaks can be obtained when analyzing Phenol or Salicylic Acid. However, as Brilliant Blue FCF has three sulfonic groups in its chemical structure, tailing will occur when the surface of the packing material is slightly basic.
Hinokitiol is a strong chelating compound, which coordinately binds with the
surface of residual trace metal impurities, resulting in severe tailing.
However, the peak shape improves as the injection increases since the surface of
the packing material of the adsorption active sites eventually become masked.
Conditions
Eluent :A) CH3CN
B) 0.1% H3PO4
A/B = 25/75
Flow rate : 0.2 mL/min
Col. Temp. : 40 ℃
Detection : UV 254 nm
Sample : 1:Brilliant Blue FCF 2:Phenol
3:Salicylic acid
Testing Procedure:
1) 100 % water is introduced into column over 20 minutes.
2) Conduct Analysis (Upper chromatogram in the following pages)
3) Stop flow for 15 minutes.
4) 100 % water is introduced again into column over 30 minutes.
5) Stop flow for 15 minutes again.
6) Conduct Analysis (Lower chromatogram in the following pages)
When analyzing hydrophilic compounds under water rich mobile phase condition,
once the pump is stopped, the hydrophobic bonded group pushes the aqueous mobile phase out off the pore in an irreversible fashion, in what has become known as the dewetting phenomenon.
Conditions
Eluent : 100% H2O
Flow rate : 0.2 mL/min
Col. Temp. : 40 ℃
Detection : UV 254 nm
Sample : 1:Cytosine 2:Uracil
3:Guanine 4:Thymine
5:Adenine
Acidic Compound Test
Chelating Compound Test
Dewetting Test
1. Brilliant Blue FCF
1. Hinokitiol
Explanation of Analytical Tests and Conditions
Notes: 4

## Slide 5
Hydrophobicity Test
L-column2 ODS
Maintenance rate of retentivity
49.9 %
CAPCELL PAK C18 MGⅢ
YMC-Triart C18
Maintenance rate of retentivity
97.5 %
InertSustain C18
1
2
3,4
5
1
2
5
3
4
6
1
2
5
3
4
1
2
3
1
1
2
5
3
4
6
1
2
5
3
4
6
1
2
5
3
4
6
1
2
5
3
4
1
2
5
3
4
1
2
5
3
4
1
2
3
5
4
Elution pattern reverses as sample 1, 2, 3, 5 are eluting later.
1
2
3,4
5
1
2
3,4
5
2
3
1
2
3
1
2
3
1
1
1
Maintenance rate of retentivity
98.2 %
Maintenance rate of retentivity
82.4 %
Dextromethorphan
Clemastine
Dextromethorphan
1. B.B.FCF
No peak
Hinokitiol
Hinokitiol
B.B.FCF
Hinokitiol
1: Uracil
2～6: Alkylbenzene
(Toluene～ n-Amylbenzene)
1: Uracil 2: Pyridine
3: Phenol
4: Berberine chloride
5: Dextromethorphan
1: Chlorpheniramine
2: Triprolidine
3: Homochlorcyclizine
4: Hydroxyzine
5: Clemastine
1: Brilliant Blue FCF 2: Phenol
3: Salicylic acid
1: Hinokitiol
Basic Compound Test (1)
Basic Compound Test (2)
Acidic Compound Test
Chelating Compound Test
Dewetting Test
Notes: 5

## Slide 6
1
2
3
4
5
1
2
3
4
5
1
2
3
Maintenance rate of retentivity
13.5 %
Maintenance rate of retentivity
95.2 %
Maintenance rate of retentivity
42.1 %
1
2
3,4
5
1
2
5
3
4
6
1
2
5
3
4
1
2
3
1
1
2
5
3
4
6
1
2
5
3
4
1
2
5
3
4
6
1
2
5
3
4
1
2
3
1
2
5
3
4
1
2
3
1
2
3
4
5
3 and 4 eluting reversely
1
2
5
3
4
6
Dextromethorphan
Dextromethorphan
Clemastine
Hinokitiol
1. No peak
Clemastine
B.B.FCF
B.B.FCF
1: Uracil
2～6: Alkylbenzene
(Toluene～ n-Amylbenzene)
1: Uracil 2: Pyridine
3: Phenol
4: Berberine hydrochloride 5: Dextromethorphan
1: Chlorpheniramine
2: Triprolidine
3: Homochlorcyclizine
4: Hydroxyzine
5: Clemastine
1: Brilliant Blue FCF 2: Phenol
3: Salicylic acid
1: Hinokitiol
Cadenza CD-C18
Gemini-NX 3u C18 110A
Luna 3u C18(2)
Maintenance rate of retentivity
82.4 %
Hydrophobicity Test
Basic Compound Test (1)
Basic Compound Test (2)
Acidic Compound Test
Chelating Compound Test
Dewetting Test
Hinokitiol
1. No peak
3 and 4 eluting reversely
Hinokitiol
1. No peak
Notes: 6

## Slide 7
InertSustain C18
1
2
3,4
5
1
2
5
3
4
6
1
2
5
3
4
1
2
3
1
3
Maintenance rate of retentivity 95.9 %
Maintenance rate of retentivity
76.8 %
Maintenance rate of retentivity
27.1 %
1
5
3
4
6
2
1
5
3
4
6
2
1
5
3
4
6
2
2
5
3
4
1
2
5
3
4
1
2
5
3
4
1
1
2
5
3
4
1
2
5
3
4
1
2
5
3
4
1
2
3
2
1
2
3
1
1: Uracil
2～6: Alkylbenzene
(Toluene～ n-Amylbenzene)
1: Uracil 2: Pyridine
3: Phenol
4: Berberine hydrochloride 5: Dextromethorphan
1: Chlorpheniramine
2: Triprolidine
3: Homochlorcyclizine
4: Hydroxyzine
5: Clemastine
1: Brilliant Blue FCF 2: Phenol
3: Salicylic acid
1: Hinokitiol
X SELECT CSH C18
XBridge C18
ZORBAX Eclipse Plus C18
Hinokitiol
Salicylic acid
Dextromethorphan
Clemastine
B.B.FCF
Clemastine
Dextromethorphan
Maintenance rate of retentivity
82.4 %
Hydrophobicity Test
Basic Compound Test (1)
Basic Compound Test (2)
Acidic Compound Test
Chelating Compound Test
Dewetting Test
3 and 4 eluting reversely
1. B.B.FCF
No peak
Hinokitiol
1. No peak
Hinokitiol
1. No peak
3 and 4 eluting reversely
Notes: 7

## Slide 8
Maintenance rate of retentivity
94.8 %
Maintenance rate of retentivity
98.2 %
InertSustain C18
1
2
3,4
5
1
2
5
3
4
6
1
2
5
3
4
1
2
3
1
1
2
5
3
4
6
1
2
5
3
4
6
1
2
5
3
4
1
2
5
3
4
1
2
5
3
4
1
2
5
3
4
1
1
2
3
2
3
1: Uracil
2～6: Alkylbenzene
(Toluene～ n-Amylbenzene)
1: Uracil 2: Pyridine
3: Phenol
4: Berberine hydrochloride
5: Dextromethorphan
1: Chlorpheniramine
2: Triprolidine
3: Homochlorcyclizine
4: Hydroxyzine
5: Clemastine
1: Brilliant Blue FCF 2: Phenol
3: Salicylic acid
1: Hinokitiol
Inertsil ODS-3
Inertsil ODS-4
Salicylic acid
Dextromethorphan
Clemastine
Clemastine
Dextromethorphan
100% aqueous mobile phase can be used by periodically flushing the column with an organic solvent.
Maintenance rate of retentivity
82.4 %
Hydrophobicity Test
Basic Compound Test (1)
Basic Compound Test (2)
Acidic Compound Test
Chelating Compound Test
Dewetting Test
3 and 4 eluting reversely
3 and 4 eluting reversely
Hinokitiol
1. No peak
1. B.B.FCF
No peak